## Slide 1: EML 4551C SENIOR DESIGN DR. KAMAL AMIN TEAM 4: ALTERNATE MATERIAL SELECTION FOR COMPRESSOR CASING IN TURBOCHARGER MIDTERM I: CONCEPT DEVELOPMENT PRESENTATION Group Members alexander Mankin HARRISON MCLARTY Ralph Scott Abiodun OLUWALOWO Project sponsor AND FACULTY Adviser Cummins - Roger England DR. PETER KALU 24 OCTOBER 2013

## Slide 2: Outline
Project Scope
Project Background
Project Objectives
Design Concepts and Evaluation
Potential Challenges and Risks
Brief Future Plans Outline
Gantt Chart
Final Summary
References
Questions

## Slide 3: Project Scope
Fig.1: View of turbocharger.[5]
Cummins has an interest in researching and selecting alternate materials to fabricate compressor casings in their B series turbochargers
This alternate material should ultimately be more cost effective than the current one in use, cast aluminum 356, and still satisfy the design and operational parameters set by Cummins
Estimates of manufacturing costs for this alternate material and 3 full scale prototypes are key requirements
Ralph Scott

## Slide 4: Project Background
Figure 1. Schematic of how a turbocharger operates
Ralph Scott

## Slide 5: Project Background cont.
A cost efficient material which could replace cast aluminum 356 presents many beneficial opportunities for Cummins
The revenue gained from more cost efficient materials and manufacturing processes present financial advantages for Cummins
Production numbers on compressor casings and turbochargers have the potential to grow allowing the company to meet and exceed the expectations of customers
Ralph Scott

## Slide 6: Project Objectives
Determine the temperatures, pressures, and stresses experienced by the compressor during operation
Research and compare materials which can operate under these prescribed physical conditions, and are cheaper both as a material and to manufacture
Estimate manufacturing costs with this new material and compare it to cast aluminum 356, which is currently used to fabricate the casings
With the known operational conditions and alternate material known, utilize Finite Element Analysis in conjunction with a CAD model of the casing for analysis
Obtain three prototypes of these casings for testing and experimentation
Ralph Scott

## Slide 7: Design Concepts
Operational Conditions for Compressor
Figure 2. Experimental data of turbocharger supplied by sponsor
Ralph Scott

## Slide 8: Design Concepts cont.
Design Specifications
Casing must possess the same design and geometric tolerances currently in place on the compressor in Cummins turbocharger
Alternate material must be able to safely and continuously operate at temperatures up to 230
Also, based on the data provided by the sponsor, the casing should be able to withstand pressures up to 215 kPa
Ralph Scott

## Slide 9: Design Concepts cont.
Performance Specifications
Material must be able to withstand cyclic temperatures including below freezing atmospheric conditions
Compressor casing must be able to withstand and contain a catastrophic failure of the compressor blades caused by over boosting, without fracturing
Corrosion resistance is also an important requirement due to the presence of oil, dirt, water, engine coolant, salt, and other chemicals during the operation of an automobile
Ralph Scott

## Slide 10: Design Concepts cont.
Why replace the current Aluminum alloy?
Reduce the overall cost of production with a cheaper alternative
Reduce the overall operating cost
Reduce the weight of the casing
Ralph Scott

## Slide 11: Design Concepts cont.
Figure 3. Properties of cast aluminum 356. (3)
Ralph Scott

## Slide 12: Design Concepts cont
Possible Material Candidates
Polymers
Thermoplastics
Thermosetting Plastics
Fiber-Reinforced Polymers(FRP)
Ceramics
Ceramic Matrix Composites(CMCs)
Metals
Magnesium
Metal Matrix Composites(MMCs)
Alex Mankin

## Slide 13: Design Concepts cont.
Tensile Strength, Yield: >= 124 MPa
Elongation @ Break: >= 3.0%
Hardness, Brinell: 45-75 (500g 10mm ball)
Solidus/ Max Operating Temp.: 557°C
Machinability: 50% (from 0-100)
Aluminum 356
Tensile Strength, Yield: 120 MPa
Elongation @ Break: 19-20%
Izod Impact: .750 J/cm
Continuous Operating Temp.: 230°C
Machinability: N/A
Deflection Temp. (264 psi): 231°C
Extem UH
Alex Mankin

## Slide 14: Design Concepts cont.
Can Operate at the required 230°C max temperature
Performs well below 0 to 230°C
Highly chemical resistant
Tensile strength is almost equal to that of aluminum 356
Advantages
Extem UH
Limitations
Unknown cost of the material
At any temperatures higher than 257°C it will start to soften
Will require a different manufacturing method than that of the aluminum
Alex Mankin

## Slide 15: Design Concepts cont.
Tensile Strength, Yield: >= 124 MPa
Elongation @ Break: >= 3.0%
Hardness, Brinell: 45-75 (500g 10mm ball)
Solidus/ Max Operating Temp.: 557°C
Machinability: 50% (from 0-100)
Aluminum 356
Tensile Strength, Yield: 7.58 MPa
Elongation @ Break: 30%
Izod Impact: .481 J/cm
Continuous Operating Temp.: 260°C
Machinability: 2 (from 1-10)
Deflection Temp. (264 psi): 132°C
Fluorosint 500
Alex Mankin

## Slide 16: Design Concepts cont.
Can operate at a continuous temperature of 260°C
Has a thermal expansion rate close to aluminums
Non-abrasive to most mating materials
Good wear characteristics
Easy to machine
Advantages
Limitations
Much lower Tensile strength compared to aluminum 356
High cost estimate
Currently can only be ordered in thin sheets or tubes
Will require a different manufacturing method due to shape of material available
Fluorosint 500
Alex Mankin

## Slide 17: Design Concepts cont.
Tensile Strength, Yield: >= 124 MPa
Elongation @ Break: >= 3.0%
Hardness, Brinell: 45-75 (500g 10mm ball)
Solidus/ Max Operating Temp.: 557°C
Machinability: 50% (from 0-100)
Aluminum 356
Tensile Strength, Yield: 186 MPa
Elongation @ Break: 1.1%
Izod Impact: .481 J/cm
Continuous Operating Temp.: 260°C
Machinability: N/A
Deflection Temp. (264 psi): 316°C
PEEK - 30% Carbon-Filled
Alex Mankin

## Slide 18: Design Concepts cont.
Can operate at a continuous temperature of 260°C
Excellent impact, and tensile characteristics
Exceptional chemical resistance
Outstanding wear and abrasion resistance
Low smoke and toxic gas emissions
Advantages
Limitations
Is the most brittle of the materials with a elongation of only 1.1%
May be more difficult to machine due to its brittleness
PEEK - 30% Carbon-Filled
Alex Mankin

## Slide 19: Design Concepts cont.
Tensile Strength, Yield: >= 124 MPa
Elongation @ Break: >= 3.0%
Hardness, Brinell: 45-75 (500g 10mm ball)
Solidus/ Max Operating Temp.: 557°C
Machinability: 50% (from 0-100)
Aluminum 356
Tensile Strength, Yield: 20.7 MPa
Elongation @ Break: 20%
Izod Impact: N/A
Continuous Operating Temp.: 288°C
Machinability: N/A
Deflection Temp. (264 psi): N/A
Rulon 945
Alex Mankin

## Slide 20: Design Concepts cont.
Can operate at a continuous temperature of 288°C
Low deformation under load and high impact resistant
Excellent abrasion and corrosion resistance
Advantages
Limitations
A low Tensile Strength to that of aluminum
Will require a different manufacturing method than that of the aluminum
Rulon 945
Alex Mankin

## Slide 21: Potential Challenges and Risks
Running into cost issues with any of the materials we choose
Finding a Machinist or company that would be willing and able to machine a prototype compressor casing out of the material we eventually decide on
Once the prototype is made, having it put under proper testing to evaluate its performance
Alex Mankin

## Slide 22: Future Plans
Final selection of material
Prototyping and testing
Determine type of manufacturing process
Determine cost for material and manufacturing process
Alex Mankin

## Slide 23: Gantt Chart
Alex Mankin

## Slide 24: Final Summary
Our task is to come up with an alternative material for a turbocharger compressor casing
Using the operating conditions provided to us by Cummins we can determine which materials are suitable
We have researched many different materials that met our criteria
We found that polymers were the best option to reduce cost and weight
No choice yet, more research is needed
Alex Mankin

## Slide 25: References
1. "Turbo Torque." Turbo Torque. N.p., n.d. Web. 21 Oct. 2013. <http://www.mazdarotary.net/turbo.htm>.
2. "Online Materials Information Resource - MatWeb." Online Materials Information Resource - MatWeb. N.p., n.d. Web. 21 Oct. 2013. <http://www.matweb.com/>.
3. "Plastic Sheet, Plastic Rod, Plastic Tubing - Buy Online." Plastic Sheet, Plastic Rod, Plastic Tubing - Buy Online. N.p., n.d. Web. 21 Oct. 2013. <http://www.professionalplastics.com/>.

## Slide 26: Questions