## Slide 1: EML 4551C SENIOR DESIGN DR. KAMAL AMIN TEAM 4: ALTERATE MATERIAL SELECTION FOR COMPRESSOR CASING IN TURBOCHARGER MIDTERM II: Interim Design PRESENTATION Group Members alexander Mankin HARRISON MCLARTY Ralph Scott Abiodun OLUWALOWO Project sponsor AND FACULTY Adviser Cummins - Roger England DR. PETER KALU 21 November 2013

## Slide 2: Outline
Project Scope
Project Background
Project Objectives
Design Concepts and Evaluation
Analytical Model
Design Analysis
Procurement of Resources
Future Work
Final Summary
References
Questions

## Slide 3: Project Scope
Fig.1: View of turbocharger.[5]
Cummins has an interest in researching and selecting alternate materials to fabricate compressor casings in their B series turbochargers
This alternate material should ultimately be more cost effective than the current one in use, cast aluminum 356, and still satisfy the design and operational parameters set by Cummins
Estimates of manufacturing costs for this alternate material and 3 full scale prototypes are key requirements
Abiodun Oluwalowo

## Slide 4: Project Background cont.
A cost efficient material which could replace cast aluminum 356 presents many beneficial opportunities for Cummins
The revenue gained from more cost efficient materials and manufacturing processes present financial advantages for Cummins
Production numbers on compressor casings and turbochargers have the potential to grow allowing the company to meet and exceed the expectations of customers
Abiodun Oluwalowo

## Slide 5: Project Objectives
Determine the temperatures, pressures, and stresses experienced by the compressor during operation
Research and compare materials which can operate under these prescribed physical conditions, and are cheaper both as a material and to manufacture
Estimate manufacturing costs with this new material and compare it to cast aluminum 356, which is currently used to fabricate the casings
With the known operational conditions and alternate material known, utilize Finite Element Analysis in conjunction with a CAD model of the casing for analysis
Obtain three prototypes of these casings for testing and experimentation
Abiodun Oluwalowo

## Slide 6: Design Concepts
Operational Conditions for Compressor
Figure 2. Experimental data of turbocharger supplied by sponsor
Abiodun Oluwalowo

## Slide 7: Design Concepts cont.
Design Specifications
Casing must possess the same design and geometric tolerances currently in place on the compressor in Cummins turbocharger
Alternate material must be able to safely and continuously operate at temperatures up to 230
Also, based on the data provided by the sponsor, the casing should be able to withstand pressures up to 215 kPa
Abiodun Oluwalowo

## Slide 8: Design Concepts cont.
Performance Specifications
Material must be able to withstand cyclic temperatures including below freezing atmospheric conditions
Compressor casing must be able to withstand and contain a catastrophic failure of the compressor blades caused by over boosting, without fracturing
Corrosion resistance is also an important requirement due to the presence of oil, dirt, water, engine coolant, salt, and other chemicals during the operation of an automobile
Abiodun Oluwalowo

## Slide 9: Design Concepts cont.
Why replace the current Aluminum alloy?
Reduce the overall cost of production and manufacturing with an alternative material
Abiodun Oluwalowo

## Slide 10: Design Concepts: Materials
Original Materials Researched
Reasons for Applicability
Only PEEK and Extem XH proved to be able to meet the demands and requirements of being a suitable compressor casing material.
Both Fluorsosint 500 and RULON 945 were not suitable do to the fact that they cannot be purchased in a large enough block to properly machine a compressor casing out of. As well as they were not able to withstand the loads associated with the turbocharger compressor casing.
Harrison McLarty

## Slide 11: Design Concepts; Materials
New Materials Researched
Reasons for Applicability
Of the new material candidates, only TECAPEEK ST and TECATOR T 15013 where deemed suitable for use in the turbocharger compressor casing.
The Material TECASINT 2000, is not applicable for our use do to the fact that it cannot be molded due to the absence of a softening point hence processed via sintering. It is also prone to hydrolysis upon contact with alkaline fluid of high pH.
TECAPEI & FORTUS PPSF cannot withstand the peak temperature of 230°C.
Harrison McLarty

## Slide 12: Design Concepts; Materials
The complete list of approved materials so far
Harrison McLarty

## Slide 13: Analytical Model: FEA of Compressor Casing
Figure 3. TECAPEEK ST
Figure 4. PEEK UNFILLED
FEA of the piping was done on a cross section of the casing to evaluate material selection
Found that almost no deformation occurred under highest operating pressure
Harrison McLarty

## Slide 14: Analytical Model: FEA of Compressor Casing
Figure 3. EXTEM XH
Figure 4. TECATOR T 15013
TECATOR T 15013 had the least displacement and TECAPEEK ST has the most displacement of materials analyzed
All materials had similar displacements and are viable options for use
Harrison McLarty

## Slide 15: Design Analysis: Decision matrix for prototype
Fig. 5 A weighted decision matrix for selecting the material used for machining a prototype
Harrison McLarty

## Slide 16: Design Analysis: Material for prototype
With the aid of a weighted decision matrix PEEK (unfilled) was found to be the most effective material for fabricating a compressor casing
It possesses the following advantages and superior characteristics:
    Heat resistance at temperatures beyond 230
    Pressure resistance ( resistance to deformation due to pressure)
    Resistance to diesel engine fluids
    Dimensional stability (i.e. low rate of water absorption)
    Excellent balance of yield strength and elongation
Harrison McLarty

## Slide 17: Design Analysis: Need for prototype
Fig.6 Example of a burst containment test. [5]
“Burst” occurs when the centrifugal force undergone by impeller wheels, due to their rotational speed, overcome the mechanical strength of the wheel.
Causes of a burst event include:
  Reduction of strength due to high internal stresses associated with high temperatures and speeds
  Fatigue failure due to cyclic loading (i.e. stop and go motion of a city bus)
  Foreign object damage (FOD) (i.e. a rock or piece of rubber impacting a wheel
Although a rare event, this must be kept in mind when selecting materials for either the compressor or turbine housing due to the safety concern of burst.
Materials with the proper yield strength, % elongation (ductility), and maximum operational temperature must be considered to withstand this event.
Harrison McLarty

## Slide 18: Status of procurement and resources
Contact at Cummins is procuring a volume block of PEEK from Victrex. Volume is approximately 10.5 in x 5.25 in x 8.5 in
Machining of the material will be completed through use of resources at Cummins.
Victrex specializes in PEEK polymers (polyaryletherketones)
If deemed suitable, the compressor casings would be manufactured on a large scale through injection molding.
Harrison McLarty

## Slide 19: Future work
Obtaining manufacturing costs through the use injection molding and comparing this to the cost of the current casting solution of aluminum 356.
Modeling burst containment through FEA and comparing this to experimental data obtained from prototype testing.
Harrison McLarty

## Slide 20: Final summary
Prototype material has been selected and is going to machined to the dimensions and tolerances of the current compressor casings used by Cummins.
Prototype testing will be carried out next semester as well as manufacturing costs associated with the PEEK material used to construct the compressor casings
Harrison McLarty

## Slide 21: References
1. "Turbo Torque." Turbo Torque. N.p., n.d. Web. 21 Oct. 2013. <http://www.mazdarotary.net/turbo.htm>.
2. "Online Materials Information Resource - MatWeb." Online Materials Information Resource - MatWeb. N.p., n.d. Web. 21 Oct. 2013. <http://www.matweb.com/>.
3. "Plastic Sheet, Plastic Rod, Plastic Tubing - Buy Online." Plastic Sheet, Plastic Rod, Plastic Tubing - Buy Online. N.p., n.d. Web. 21 Oct. 2013. <http://www.professionalplastics.com/>.
4. "VICTREX® PEEK Polymers." High Performance Polyaryletherketones, High Temperature Advanced PEEK Polymer, Thermoplastic. N.p., n.d. Web. 19 Nov. 2013. <http://www.victrex.com/en/products/victrex-peek-polymers/victrex-peek-polymers.php>.
5. "Burst and Containmnet: Ensuring Turbocharger Safety." Turbobygarrett.com. N.p., n.d. Web. 19 Nov. 2013. <http://www.turbobygarrett.com/turbobygarrett/sites/default/files/Garrett_White_Paper_02_Burst__Containment.pdf>.
Harrison McLarty

## Slide 22: Questions
Harrison McLarty