Growth and Properties of (BaTiO3)n/(SrTiO3)m Superlattices: Study of Nanoscale Ferroelectricity

X. X. Xi

Materials Research Institute, Department of Physics, and Department of Materials Science and Engineering, The Pennsylvania State University, University Park, Pennsylvania

The advance in oxide thin film technology has allowed growth of nanoscale oxide ultrathin films and heterostructures, which provides new opportunities for nano-science and novel applications. We have demonstrated the growth of BaTiO3/SrTiO3 superlattices on SrTiO3 substrates by reactive molecular-beam epitaxy, which showed high structural quality with nearly atomically abrupt interfaces. In bulk, BaTiO3 is ferroelectric below 403 K and SrTiO3 is quantum paraelectric. Using ultraviolet Raman spectroscopy we showed that one-unit-cell-thick BaTiO3 layers in BaTiO3/SrTiO3 superlattices are not only ferroelectric (with Tc as high as 250 kelvin) but also polarize the quantum paraelectric SrTiO3 layers adjacent to them. Tc was tuned by ~500 kelvin by varying the thicknesses of the BaTiO3 and SrTiO3 layers, revealing the essential roles of electrical and mechanical boundary conditions for nanoscale ferroelectricity.

This seminar will be held in A226 at 11:00am.